## Slide 1: 2. Theory of Original Cam Clay (OCC)
Mike Jefferies, PEng
Dr. Dawn Shuttle, PEng
January, 2015

## Slide 2: Why theory ?
Looked at soil behaviour from effective stress and drained data
But, what about undrained ?
    Why do pore pressures develop ?
Want to understand how the basic properties control the stress-strain behaviour
    Effect of void ratio
    Transition into static liquefaction
Need to move from the laboratory to insitu…
    How to we evaluate insitu tests ?

## Slide 3: Theory of Plasticity
Applies to all materials… steel, copper, pvc, concrete. And soil.
    Understanding how materials deform
Based on some simple ideas that you can observe for yourself
Greatest contribution to applied mechanics of the 20th century
There is a paper on the history of plasticity theory in the folder ‘Light Reading’

## Slide 4: Plastic strains
Elastic
Plastic
e = ep + ee
[Tresca, 1884]
Applies to all strains

## Slide 5: Undrained behaviour
Undrained: impose e = constant (thus, no volumetric strain)
Effective stress definition:
Elastic-plastic strain decomposition
Add volumetric elasticity
s ′= s - u  ds ′ = ds - du

## Slide 6: Effect of plasticity in undrained loading

## Slide 7: Components of plasticity theory
Yield surface
Flowrule …analogue to Poisson’s Ratio
    Normality
Hardening (and softening) Law …analogue to Young’s Modulus
    Depends on plastic distortional strain increment
Elasticity
    Both within and on yield surface
    Constant n seems appropriate, G & K = f(e,s)

## Slide 8: Yield surface
s1
s2
s3
Elasticity
Yield Surface

## Slide 9: Flow rule (relative amount of plastic strain increments)
s1 de1
s2
de2
s3 de3
Elasticity
Plasticity equivalent of Poisson’s Ratio
Work conjugate

## Slide 10: Hardening
s1 de1
s2
de2
s3 de3
Elasticity
YS changes location
YS changes shape
YS changes size
Elasticity
Plastic strain

## Slide 11: Consistency
s1 de1
s2
de2
s3 de3
Elasticity
Elasticity

## Slide 12: “Normality” (associated flow rule)
P2 > P1

## Slide 13: “Normality” = Associated Flow Rule
THEOREM

## Slide 14: Development of plasticity theory
Plasticity theory introduced to soil mechanics ~ 1945
Soils change volume with distortion
Soil strength and stiffness depends on mean stress
Dreadnought 1906

## Slide 15: Appropriate plasticity theory for soils: 1945
Mohr-Coulomb ‘strength’
Elastic

## Slide 16: Appropriate plasticity theory for soils: 1950
NAMC
Elastic

## Slide 17: Appropriate plasticity theory for soils: 1957
Hvorslev surface
Critical state friction ratio
Oedometer path

## Slide 18: Drucker, Gibson & Henkel: 1957 (Conceptual)
Hvorslev surface
Critical state

## Slide 19: Math that computes: Original Cam Clay (OCC)
Critical state locus (CSL)
    Semi-log form: G, l
Critical state friction
    Stress ratio: M
Elasticity
    Volumetric semi-log form: k
Convention: Greek symbols used for properties in CSSM
Idealizations (models): named after your local body of water
1968

## Slide 20: PROPERTIES: Isotropic compression
Void ratio
Mean effective stress, p’: kPa
cc
l10
G
Spacing Ratio = picl / pcsl

## Slide 21: PROPERTIES: Elasticity
Void ratio
Mean effective stress, p’: kPa
cc
cs,r

## Slide 22: Log10 versus Ln
CSL: ec= G - l ln(p’)
Elasticity: de = k dp′ / p ′
CSL: ec= G - l10 log(p’)
Elasticity: De = cr log( pold / pnew)
Used in theory (ln)
What the lab reports (log)
l = l10 / 2.3 k = cr / 2.3

## Slide 23: PROPERTIES: Critical Friction Ratio
Deviator stress, q: kPa
Mean effective stress, p’: kPa

## Slide 24: Basis of Original Cam Clay
Postulates
    Simple physical idealizations
    Inspired by test data, but do not depend on data to justify
Consistent and formal mathematics
At the end discuss “utility” of OCC by looking at how well the theory explains what we observe/measure

## Slide 25: Derive the OCC flowrule
Work:
s1
s2 , s3
s1+Ds1
s2 , s3
Consider a unit volume element of soil loaded by a strain increment...

## Slide 26: Plastic work dissipated by soil skeleton
Use elastic-plastic strain decomposition:
Divide this plastic work rate first by the mean effective stress (to make it dimensionless);
Divide by the plastic shear strain increment (normalized rate of working per unit plastic distortion of the soil)...
“universally acknowledged truth” (no constitutive model)
DWp = DW – DWe = q Deqp + p Devp
DWp/(p Deqp ) = q / p + Devp/Deqp = h + Dp
Normalized rate of dissipation of plastic work (into heat)
Stress-dilatancy

## Slide 27: The OCC idealization
Postulate: (model)
Universally known truth:
Flowrule (Stress-Dilatancy)

## Slide 28: “Normality” = Associated Flow Rule
devp
THEOREM
deqp
Dp
Dq
devp
deqp
Dp =devp / deqp

## Slide 29: High-school geometry...
X
- 1 /X
dp/dq = - 1/Dp
Invoke normality:

## Slide 30: Getting to YS: a bit of math...
Definition... q = h p
Differentiate... dq = p dh + h dp
Eliminate dq.. dq = - dp Dp from normality - dp D = p dh + h dp dp /p + dh / (D+h) = 0

## Slide 31: Derivation of OCC yield surface
From normality...
From plastic working...
Combine...
And integrate...
M = Dp + h
ln(p) + h/M = C

## Slide 32: Choice of integration term “C”
D = 0
M
pc

## Slide 33: How does void ratio control strength ?
e
ln(p)
l
k
Notes: Substitute for pc in 1-eta/M = ln(p/pc)

## Slide 34: OCC – the equations
Yield surface:
Flowrule:
Hardening:
Elasticity:
Only 4 soil properties… G, l, k, M
Normality & Work
Work
CSL

## Slide 35: “state boundary surface”
=1+e
Barking mad view ! And where is plastic strain ?
Combine yield surface with hardening law

## Slide 36: Let us do hardening properly…
ln(p)
CSL
A
B
l
k
void ratio, e
Plastic void ratio change
dep = - (l- k) dpc / pc

## Slide 37: Strain-induced hardening…
Plastic void ratio change:
Strain to void ratio……
PLASTIC HARDENING:
H
dep = - (l- k) dpc / pc

## Slide 38: Consistency condition
Stresses must remain on yield surface during plastic yield
Hardening Law

## Slide 39: Standard ideas for consistency
Yield surface: F(s, e, z...) = 0
    If F < 0 then ‘elastic’
    If F=0 then ‘plastic’
    F>0 not admissible
CONSISTENCY CONDITION
    Must remain on the yield surface during yielding
    mathematically: dF = 0
Rewrite OCC yield surface as:

## Slide 40: Consistency condition for OCC
For yield surface written as F=0, consistency is dF=0
Use with...
Hardening Law
Loading path

## Slide 41: Consistency in undrained yielding

## Slide 42: OCC – the equations
Flowrule:
Hardening:
Consistency:
Elasticity:
Only 4 soil properties… G, l, k, M
Normality & Work
Work
CSL

## Slide 43: EXERCISE 2: Compute undrained OCC
Folder ‘Exercise Templates’: OCC_CIU_EX2_template.xls
Compute q vs e and p-q
Compare with closed-form

## Slide 44: OCC_CIU_EX2.xls

## Slide 45: Integration: how ?
OCC is incremental:
    How does pc change with strain ?
    Where is the stress state on the yield surface ?
No closed form solutions in CSSM (mostly)…. NUMERICS
General situations
    stress, strain, state varies across loaded body
    finite element or finite differences
Laboratory tests
    “element” tests with soil at “uniform” stress and strain state
    stress or strain paths controlled by test arrangement (txl : Dq= 3 Dp)
    allows direct numerical integration of plasticity model

## Slide 46: Euler basics – what your xls will do…
1748

## Slide 47: Integration loop
Get state variables … G, K, Mi depend on (e, s)
(eqp)NEW= (eqp)OLD + Deqp … step forward plastic strain step
Apply flowrule => Devp … the other strain increment
Harden yield surface ... yield surface changes size
Find new stress state … depends on stress path
Add elastic strain incs
Update e
Repeat until done

## Slide 48: The Integration “Loop”
End of one step becomes start for the next

## Slide 49: Use ‘named’ variables for properties

## Slide 50: Soil Property Inputs
k = l /4

## Slide 51: Initial void ratio for isotropic test…

## Slide 52: Initial size of the yield surface (isotropic)

## Slide 53: Getting units correct
People need information presented in familiar forms
    Avoids errors !
    For engineers, allows instinctive reality checks
    The templates you will use follow this protocol
Equations must be in consistent units
    Some inputs in MPa but calculate throughout in kPa
    Make unit conversions explicit

## Slide 54: Unit conversion…
MPa_to_kPa

## Slide 55: Verification and Validation
Verification: does the numerical model compute correctly ?
    Compare numerical solution with a reference solution
    Reference solution ideally closed form (but very few of them)
    Cannot verify numerical methods by laboratory testing
Validation: does the verified model have any relevance to engineering reality ?
    Compare model with a body of laboratory test data…
    Back-analysis of case-histories (but rarely know enough…)

## Slide 56: Verification of OCC implementation
http://www.geotechnique.info/
  Chapter 6 in workshop info files
OCC has two closed form solutions
    Constant-p CID for NC soil
    Undrained CIU for NC soil
Use published solution without derivation
Solution in Section 6.7
    Implicit
    Need to use 3 equations

## Slide 57: OCC solution for CIU test on NC soil

## Slide 58: Verification result… perfection
Numerical using Euler integration
Closed form S&W Sect 6.7

## Slide 59: Intergation sequence in the worksheet
equations in the hand-out !

## Slide 60: Your turn !
This is the hardest part of this course…

## Slide 61: OCC – the equations
Flowrule:
Hardening:
Consistency:
Elasticity:
Only 4 soil properties… G, l, k, M
Normality & Work
Work
CSL
H
G = 2000 MPa

## Slide 62: OCC – the equations
Yield surface:
Flowrule:
Hardening:
Elasticity:
Undrained: dp = - K devp
Normality & Work
Work
CSL
H